# TECHNICAL DATA SHEET

350 Series

Floor & Deck Enamel

100% Acrylic

Mildew & Stain Resistant Finish

Specially formulated for the Florida climate

__________________________________________________________________________________________

Povia 350 100% Acrylic Floor & Deck Enamel is a versatile and durable coating which produces a hard, tough, protective finish.  Povia 350 exhibits excellent adhesion, hot tire resistance, easy application and maximum performance on both wood and concrete floors.

__________________________________________________________________________________________

RECOMMENDED USES:

For properly prepared concrete patios, walkways, pool decks, asphalt, driveways, garage floors, wood decks and composite decking.  FOR INTERIOR AND EXTERIOR USE!  Do not apply to smooth troweled concrete floors without proper preparation.  A texture is required for sufficient adhesion.

SURFACE PREPARATION:

General: Dirt, grease, grime and any foreign material must be removed before application of new coating.  Treat surface for mildew.  Insure surface is clean and dry.  Contact a Povia Paints representative for detailed surface preparation specifications.

New or unpainted concrete: Dirt, grease, grime and any foreign material must be removed before application of new coating.  Apply a solution of 1 part muriatic acid to 3 parts water then thoroughly wash with a TSP solution or a powerful degreasing detergent.  Smooth troweled floors must be etched until pores are open and a texture is achieved.  Pressure washing is highly recommended to ensure all contaminants are removed.

Painted surfaces:  Povia 350 will adhere to most prepainted surfaces that are firmly bonded to the substrate.  Dirt, grease, grime and any foreign material must be removed before application of new coating.  Do not acid etch previously painted surfaces.  Povia 350 may not be compatible with certain types of existing finishes. Glossy surfaces should be lightly sanded prior to application.  Always check for adhesion prior to coating prepainted surfaces.

Unpainted wood surfaces: Dirt, grease, grime and any foreign material must be removed before application of new coating.

APPLICATION:

Mix product thoroughly.  Apply with brush roller or airless spray. Apply when surface temperatures are at least 50 deg. and rising.  Do not thin with paint thinners.  When spraying, use a tip designed for flat wall coatings.

RECOMMENDED THINNER:

For most applications, Povia 350 does not require thinning and should be used as is, directly from the container.  Povia 350 should be thinned with 1 pint of clean water per gallon when applying to unpainted concrete.

PRIMING INFORMATION:

New or unpainted concrete: Apply two coats Povia 350.  The first coat should be thinned with 1 pint of clean water per gallon.  The second coat should be applied undiluted.

Painted surfaces:  Primer is dependent on condition of existing coating.  Typically, two coats of Povia 350 are sufficient.  However, INSECO Multi Surface Conditioner (MSC) should be applied to deteriorating or chalking surfaces.

Unpainted wood surfaces:  Prime with Povia 023 100% Acrylic All Purpose Primer/Sealer/Stain Killer.  When priming new wood, allow primer to dry for 24-48 hours before applying Povia 350.  Finish with two coats Povia 350.

Composite decking: Contact a Povia Paints representative for detailed specifications pertaining to the type of composite decking.

TECHNICAL DATA:

Finish: Satin

Pigment Type: Titanium Dioxide and inert pigments

Vehicle Type: 100% Acrylic Copolymer

Solvent Type: Water

% Solids By Weight: 45% +/- 2%

% Solids By Volume: 35% +/- 2%

Density: 10.29 lbs. Per gallon

Viscosity @ 75 deg. F (24 deg. C): 100 +/- 2 K.U.

Coating VOC: <200 g/l

Estimated Dry Time:  To touch 30-60 minutes ; Recoat 4-6 hours

Allow at least 4 hours before recoating.  Povia 350 may be walked on after drying overnight.  A minimum of 72 hours is required before before driving vehicles on coating.  High humidity and/or low temperatures may extend drying and curing time.

Flash Point, Minimum: Not Flammable

Flame Spread: Class A rating on non-combustible substratum

Recommended Dry Film Thickness Per Coat: 1.0-2.0 Mils DFT.

Clean Up: Clean up drips and spills immediately using a damp cloth.  Clean tools and equipment with soap and fresh water.

Coverage (Theoretical): Coverage will depend on porosity and contour of the surface being coated.    Coverage typically averages 200-400 square feet per gallon.

Povia 350  is water based.  Do not Freeze.

CAUTION: KEEP OUT OF REACH OF CHILDREN!

WARNING! If you scrape, sand or remove old paint, you may release lead dust.  LEAD IS TOXIC.  EXPOSURE CAN CAUSE SERIOUS ILLNESS, SUCH AS BRAIN DAMAGE, ESPECIALLY IN CHILDREN.  PREGNANT WOMEN SHOULD ALSO AVOID EXPOSURE.  Wear an NIOSH-approved respirator to control lead exposure.  Carefully clean up with a HEPA vacuum and a wet mop.  Before you start, find out how to protect yourself and your family by contacting the National Lead Information Hotline at 1-800-424-LEAD or log on to www.epa.gov/lead.

Technical data contained herein is true and accurate at the date of issue, but is subject to change without notice.  A Povia Paints representative should be contacted with any questions concerning product information or application procedures.  Our products conform to Povia quality standards, but no other warranty is expressed or implied.  Liability, if any, is limited to the replacement of product or purchase price.

## Povia Paints, Inc., 5601 Banner Dr., Ft. Myers, FL 33912  239-791-0011

www.poviapaints.com