# TECHNICAL DATA SHEET

800 Series

MARINE ENAMEL

Industrial Alkyd/Urethane Gloss Enamel

Rust Inhibitive

Interior/Exterior/Mildew Resistant

Specially formulated for the Florida climate

Povia 800 MARINE ENAMEL Industrial Polyurethane Gloss Enamel  is a premium, smooth flowing, rust inhibitive, maintenance enamel that dries without brush or lap marks to a durable protective film.  Povia 800 provides superior coverage, abrasion resistance, impact resistance, salt spray resistance and resistance to chemical cleaners.  Povia 800 is VOC compliant, offers easy application and is safe for use in hospitals, factories, food processing plants, schools, government institutions and residential applications.

__________________________________________________________________________________________

RECOMMENDED USES:

For interior and exterior use on all types of properly primed and previously painted surfaces.

SURFACE PREPARATION:

Dirt, grease, grime and any foreign material must be removed before application of new coating.  Treat surface for mildew.  Be sure surface is clean and dry.  Contact a Povia Paints representative for detailed surface preparation specifications.

APPLICATION INFORMATION:

Mix product thoroughly and apply with brush, roller or airless sprayer.  When spraying, use a tip designed for gloss wall coatings.  Apply when surface and air temperatures are above 50 Deg. F.

RECOMMENDED THINNER:

Povia 800 does not require thinning use directly as supplied.

RECOMMENDED PRIMER

Drywall: 	Unpainted drywall should be primed with Povia 021 Drywall Primer.

Plaster: 	Prime with Povia 023 100% Acrylic Primer or Povia 022 100% Acrylic

Masonry Primer thinned with one (1) pint of clean water to the gallon as

a sealer.

Masonry:	New masonry surfaces should be primed with Povia 022 100% Acrylic Masonry Primer.

Previously painted masonry surfaces should be primed with Povia 010 100% Acrylic Chalk Sealer/Surface Conditioner.

Wood:	New wood should be primed with Povia 023 100% Acrylic Primer. If staining occurs, spot prime areas with Povia 050 Stain Killer Primer/Sealer. Previously painted wood should be spot tested for compatibility and adhesion to the previous coating. Glossy surfaces should be lightly sanded prior to application.

Metal:	Steel should be sanded or scraped with a wire brush to remove all rust.  Prime with a Povia 060 Rust Inhibitive Primer or an alternate primer approved by a Povia representative. Galvanized metal should be cleaned with Ospho. Rinse thoroughly with clean, fresh water. Prime with Povia 023 100% Acrylic Primer.

TECHNICAL DATA:

Finish: Gloss

Pigment Type: Titanium Dioxide

Vehicle Type: Alkyd/Urethane

Solvent Type: Mineral Spirits

% Solids By Weight: 69% +/- 2%

% Solids By Volume: 53% +/- 2%

Density: 10.08 lbs. Per gallon

Viscosity @ 75 deg. F (24 deg. C): 85 +/- 2 K.U.

Coating VOC: <400 g/l

Estimated Dry Time:  To touch 2-4 hours ; Recoat 6-8 hours

Flash Point, Minimum: 107 deg. F

Recommended Dry Film Thickness Per Coat: 1.0-2.0 Mils DFT.

Clean Up:  Mineral Spirits

Coverage (Theoretical): Coverage will depend on porosity and contour of the surface being coated.  Coverage typically averages 300-400 square feet per gallon.

Environmental & Safety Information:

Improper handling or use may be hazardous.  Recommended safety precautions for storage , handling and application must be observed.

DANGER:

COMBUSTIBLE!  KEEP OUT OF REACH OF CHILDREN!

Contains flammable solvents.  Causes eye burns.  Vapor is harmful.  May cause allergic skin reaction.  Do not get in eyes, on skin or on clothing.  Wear eye and skin protective equipment when handling.  Wear appropriate, properly fitted respirator (NIOSH.MSHA approved) during and after application unless air monitoring demonstrates vapor/mist levels are below applicable levels.  Follow respirator manufacturer’s recommendations for use.  Keep containers closed when not in use.

First Aid:  In case of eye contact, flush eyes immediately with plenty of fresh water for at least 15 minutes.  Call a physician.  If inhaled, remove to fresh air.  If not breathing, give artificial respiration, preferably mouth to mouth and seek immediate medical assistance.  In case of skin contact, wash immediately with soap and fresh water.  Remove contaminated clothing and launder before use.  Discard shoes if material has penetrated inside surface.

Notice:  Reports have associated repeated and prolonged occupational overexposure to solvent with permanent brain and nervous system damage.  Intentional misuse by deliberately concentrating and inhaling the contents may be harmful or fatal.

WARNING! If you scrape, sand or remove old paint, you may release lead dust.  LEAD IS TOXIC.  EXPOSURE CAN CAUSE SERIOUS ILLNESS, SUCH AS BRAIN DAMAGE, ESPECIALLY IN CHILDREN.  PREGNANT WOMEN SHOULD ALSO AVOID EXPOSURE.  Wear an NIOSH-approved respirator to control lead exposure.  Carefully clean up with a HEPA vacuum and a wet mop.  Before you start, find out how to protect yourself and your family by contacting the National Lead Information Hotline at 1-800-424-LEAD or log on to www.epa.gov/lead.

Technical data contained herein is true and accurate at the date of issue, but is subject to change without notice.  A Povia Paints representative should be contacted with any questions concerning product information or application procedures.  Our products conform to Povia quality standards, but no other warranty is expressed or implied.  Liability, if any, is limited to the replacement of product or purchase price.

## Povia Paints, Inc., 5601 Banner Dr., Ft. Myers, FL 33912  239-791-0011

ww.poviapaints.com