# TECHNICAL DATA SHEET

900 Series

“MASTIC”

100% Acrylic Elastomeric

HI-BUILD

Specially formulated for the Florida climate

__________________________________________________________________________________________

Povia 900 “ MASTIC” 100% Acrylic Elastomeric is a high build, waterproof finish that employs the most technologically advanced, 100% acrylic elastomeric resins available.  Povia 900 provides excellent adhesion, flexibility, durability and weather resistance.  Povia 900 is designed to provide maximum protection against wind driven rain while it’s permeable film build bridges hairline cracks and allows moisture vapors to escape from within the structure.  Povia 900 has excellent color retention and mildew resistance and is formulated to meet Federal Specification TT-C-555B for resistance to wind driven rains.

__________________________________________________________________________________________

RECOMMENDED USES:

For properly primed exterior, vertical surfaces of concrete, stucco, masonry, wood, galvanized metal and aluminum. May also be used as a premium roof coating.

SURFACE PREPARATION:

Dirt, grease, grime and any foreign material must be removed before application of new coating.  Insure surface is clean and dry.  Contact a Povia Paints representative for detailed surface preparation specifications.

APPLICATION:

Mix product thoroughly.  Apply with brush roller or airless spray. Apply when surface temperatures are at least 50 deg. and rising.  Do not thin with paint thinners.  When spraying, use a tip designed for flat wall coatings.

RECOMMENDED THINNER:

Povia 900 does not require thinning and should be used as is, directly from the container.

RECOMMENDED PRIMER

Masonry:	New masonry surfaces should be primed with Povia 022 100% Acrylic Masonry Primer.

Previously painted masonry surfaces should be primed with Povia 010 100% Acrylic Chalk Sealer/Surface Conditioner.

Wood:	New wood should be primed with Povia 023 100% Acrylic Primer. If staining occurs, spot prime areas with Povia 050 Stain Killer Primer/Sealer. Previously painted wood should be primed with Povia 010 100% Acrylic Chalk Sealer/Surface Conditioner.  Spot test previously painted wood for compatibility and adhesion to the previous coating. Glossy surfaces should be lightly sanded prior to application.

Metal:	Contact a Povia representative for specifications when applying Povia 900 to metal surfaces.  .

TECHNICAL DATA:

Finish: Satin

Pigment Type: Titanium Dioxide and inert pigments

Vehicle Type: 100% Acrylic Elastomeric Copolymers

Solvent Type: Water

% Solids By Weight: 56% +/- 2%

% Solids By Volume: 423% +/- 2%

Density: 11.10 lbs. Per gallon

Viscosity @ 75 deg. F (24 deg. C): 115 +/- 2 K.U.

Coating VOC: <200 g/l

Estimated Dry Time:  To touch 30-60 minutes ; Recoat 4-6 hours

Flash Point, Minimum: Not Flammable

Flame Spread: Class A rating on non-combustible substratum

Recommended Dry Film Thickness Per Coat: 1.5-2.5 Mils DFT.

Elongation @ 25 deg C: 340% / ASTM-D412

Water Vapor Trans: 9.6 Perms

Tensile Strength @ 25 deg C: 240 PSI / ASTM-D412

Wind Driven Rains: Meets Federal Spec TT-C-555B

Clean Up: Clean up drips and spills immediately using a damp cloth.  Clean tools and equipment with soap and fresh water.

Coverage (Theoretical): Coverage will depend on porosity and contour of the surface being coated.    Coverage typically averages 75-125 square feet per gallon.

Povia 900   is water based.  Do not Freeze.

CAUTION: KEEP OUT OF REACH OF CHILDREN!

WARNING! If you scrape, sand or remove old paint, you may release lead dust.  LEAD IS TOXIC.  EXPOSURE CAN CAUSE SERIOUS ILLNESS, SUCH AS BRAIN DAMAGE, ESPECIALLY IN CHILDREN.  PREGNANT WOMEN SHOULD ALSO AVOID EXPOSURE.  Wear an NIOSH-approved respirator to control lead exposure.  Carefully clean up with a HEPA vacuum and a wet mop.  Before you start, find out how to protect yourself and your family by contacting the National Lead Information Hotline at 1-800-424-LEAD or log on to www.epa.gov/lead.

Technical data contained herein is true and accurate at the date of issue, but is subject to change without notice.  A Povia Paints representative should be contacted with any questions concerning product information or application procedures.  Our products conform to Povia quality standards, but no other warranty is expressed or implied.  Liability, if any, is limited to the replacement of product or purchase price.

## Povia Paints, Inc., 5601 Banner Dr., Ft. Myers, FL 33912  239-791-0011

www.poviapaints.com