# TECHNICAL DATA SHEET

022 Series

Hot Stucco Primer

100% Acrylic

Pigmented Masonry Sealer

Specially formulated for the Florida climate

Povia 022 100% Acrylic Hot Stucco Primer is a resin rich, pigmented primer/sealer designed for application to new masonry surfaces.  Povia 022 is alkali resistant and may be applied to fresh stucco and masonry surfaces.  Povia 022 is highly resistant to “Hot Stucco.”

__________________________________________________________________________________________

RECOMMENDED USES:

For use on any new or uncoated masonry or plaster surface.

SURFACE PREPARATION:

Dirt, grease, grime and any foreign material must be removed before application of new coating.  Treat surface for mildew.  Be sure surface is clean and dry.  Patch all cracks and openings after application of Povia 022.

APPLICATION INFORMATION:

Mix product thoroughly and apply with brush, roller or airless sprayer.  When spraying, use a tip designed for flat wall coatings.  Apply when surface and air temperatures are above 50 Deg. F.

RECOMMENDED THINNER:

Povia 022 does not require thinning use directly as supplied.

TECHNICAL DATA:

Finish: Low Sheen

Vehicle Type: 100% Acrylic

Solvent Type: Water

% Solids By Weight: 44% +/- 2%

% Solids By Volume: 30% +/- 2%

Density: 10.30 lbs. Per gallon

Viscosity @ 75 deg. F (24 deg. C): 100 +/- 2 K.U.

Coating VOC: <150 g/l

Estimated Dry Time:  To touch 30-60 minutes ; Recoat 2 hours

Flash Point, Minimum: Not Flammable

Flame Spread: Class A rating on non-combustible substratum

Recommended Dry Film Thickness Per Coat: 1.0-2.0 Mils DFT.

Clean Up: Clean up drips and spills immediately using a damp cloth.  Clean tools and equipment with soap and fresh water.

Coverage (Theoretical): Coverage will depend on porosity and contour of the surface being coated.    Coverage typically averages 150-250 square feet per gallon.

Povia 022  is water based.  Do not Freeze.

CAUTION: KEEP OUT OF REACH OF CHILDREN!

WARNING! If you scrape, sand or remove old paint, you may release lead dust.  LEAD IS TOXIC.  EXPOSURE CAN CAUSE SERIOUS ILLNESS, SUCH AS BRAIN DAMAGE, ESPECIALLY IN CHILDREN.  PREGNANT WOMEN SHOULD ALSO AVOID EXPOSURE.  Wear an NIOSH-approved respirator to control lead exposure.  Carefully clean up with a HEPA vacuum and a wet mop.  Before you start, find out how to protect yourself and your family by contacting the National Lead Information Hotline at 1-800-424-LEAD or log on to www.epa.gov/lead.

Technical data contained herein is true and accurate at the date of issue, but is subject to change without notice.  A Povia Paints representative should be contacted with any questions concerning product information or application procedures.  Our products conform to Povia quality standards, but no other warranty is expressed or implied.  Liability, if any, is limited to the replacement of product or purchase price.

## Povia Paints, Inc., 5601 Banner Dr., Ft. Myers, FL 33912  239-791-0011

www.poviapaints.com