INSECO, Inc.

# TECHNICAL DATA SHEET

660 Series

Clear Silicone Acrylic

Concrete Waterproofing Sealer

Solvent Base

Specially formulated for the Florida climate

660 Clear Seal Silicone/Acrylic Concrete Waterproofing Sealer is a premium, silicone acrylic, penetrating, concrete sealer.  660 Clear Seal penetrates into the surface and produces a tough, durable, clear, non-yellowing, abrasion and chemical resistant film.  660 Clear Seal protects against water, UV rays, most acids, industrial chemicals, oil and grease.  660 Clear Seal also provides tremendous resistance against wear from both foot and vehicular traffic.

__________________________________________________________________________________________

RECOMMENDED USES:

For properly prepared uncoated driveways, garage floors, patios, walkways, pool decks, warehouse floors, pavers, brick, block, masonry walls and cement tile roofs.  660 Clear Seal may also be used on the underside of metal carports to prevent condensation drips from staining cars.

SURFACE PREPARATION:

For All Substrates:

Dirt, grease, grime and any foreign material must be removed before application of new coating.  Treat surface for mildew.  Oil and grease should be scrubbed with a solution of TSP and water.  Be sure surface is clean and dry.  Contact an Inseco representative for detailed surface preparation specifications.

New Concrete:

Etch with one (1) part muriatic acid to four (4) parts water.  For proper penetration and adhesion, surfaces must be etched until a porous profile is achieved.  After etching is complete, thoroughly wash with a solution of TSP and water or an alternate acid-neutralizing detergent and rinse with clean water.  Allow to dry for a minimum of 24 hours before applying 660 Clear Seal.

Pre-Painted Surfaces:

Not recommended.

APPLICATION INFORMATION:

Mix product thoroughly and apply with brush, roller or airless sprayer.  When spraying, use a tip designed for gloss coatings.  Apply when surface and air temperatures are above 50 Deg. F.  Do not apply if the threat of rain exists or if moisture or dew may condense on the surface prior to 660 Clear Seal curing.  Cover and protect all vegetation and surrounding areas not being sealed.  Do not over apply, soak the concrete or allow product to puddle.  Two thin coats are recommended for best performance. Do not apply to painted surfaces.

RECOMMENDED THINNER:

660 Clear Seal does not require thinning and should be used as is, directly from the container.

TECHNICAL DATA:

Finish: Sheen

Pigment Type:  None

Vehicle Type: 100% Acrylic Copolymer

Solvent Type: Aromatic Hydrocarbons

% Solids By Weight: 36% +/- 2%

% Solids By Volume: 30% +/- 2%

Density: 7.8 lbs. per gallon

Viscosity @ 75 deg. F (24 deg. C): 80 +/- 2 K.U.

Coating VOC: <600 g/l

Estimated Dry Time:  To touch 30-60 minutes ; Recoat 2 hours

Flash Point, Minimum: 107 deg. F

Clean Up:  Xylene

Estimated Dry Time:

Touch 			- 30-60 minutes

Recoat 		- 2 hours

Foot Traffic		- 24 Hours

Vehicular Traffic	- 72 Hours

Coverage (Theoretical): Coverage will depend on porosity and contour of the surface being coated.  Coverage typically averages 300-400 square feet per gallon.

Note: 660 Clear Seal complies with the 1999 AIM regulation category of Water Repellant Sealer that has a VOC limit of 600 g/l.  Thinning of this product will render it noncompliant.

Environmental & Safety Information:

Improper handling or use may be hazardous.  Recommended safety precautions for storage, handling and application must be observed.

DANGER:

COMBUSTIBLE!  KEEP OUT OF REACH OF CHILDREN!

Contains flammable solvents.  Causes eye burns.  Vapor is harmful.  May cause allergic skin reaction.  Do not get in eyes, on skin or on clothing.  Wear eye and skin protective equipment when handling.  Wear appropriate, properly fitted respirator (NIOSH.MSHA approved) during and after application unless air monitoring demonstrates vapor/mist levels are below applicable levels.  Follow respirator manufacturer’s recommendations for use.  Keep containers closed when not in use.

First Aid:  In case of eye contact, flush eyes immediately with plenty of fresh water for at least 15 minutes.  Call a physician.  If inhaled, remove to fresh air.  If not breathing, give artificial respiration, preferably mouth to mouth and seek immediate medical assistance.  In case of skin contact, wash immediately with soap and fresh water.  Remove contaminated clothing and launder before use.  Discard shoes if material has penetrated inside surface.

Notice:  Reports have associated repeated and prolonged occupational overexposure to solvent with permanent brain and nervous system damage.  Intentional misuse by deliberately concentrating and inhaling the contents may be harmful or fatal.

WARNING! If you scrape, sand or remove old paint, you may release lead dust.  LEAD IS TOXIC.  EXPOSURE CAN CAUSE SERIOUS ILLNESS, SUCH AS BRAIN DAMAGE, ESPECIALLY IN CHILDREN.  PREGNANT WOMEN SHOULD ALSO AVOID EXPOSURE.  Wear an NIOSH-approved respirator to control lead exposure.  Carefully clean up with a HEPA vacuum and a wet mop.  Before you start, find out how to protect yourself and your family by contacting the National Lead Information Hotline at 1-800-424-LEAD or log on to www.epa.gov/lead.

Technical data contained herein is true and accurate at the date of issue, but is subject to change without notice.  An Inseco representative should be contacted with any questions concerning product information or application procedures.  Our products conform to Inseco quality standards, but no other warranty is expressed or implied.  Liability, if any, is limited to the replacement of product or purchase price.

## Inseco, Inc., 5601 Banner Dr., Ft. Myers, FL 33912  239-939-1072

www.woodrx.com