# TECHNICAL DATA SHEET

APEX

Acrylic/Epoxy

“HIGH PERFORMANCE PROTECTIVE ENAMEL”

Self-Cross Linking/Non Yellowing

Satin Finish

4310

Specially formulated for the Florida climate

__________________________________________________________________________________________

Povia APEX Acrylic/Epoxy Satin Enamel is an alternative to traditional, one part, pre-catalyzed waterborne epoxy finishes.  Povia APEX  is an extremely durable, easy to use, single component acrylic/epoxy which offers many of the high performance characteristics expected from the traditional two component epoxies without the odor, pre-mixing, pot life and application difficulties inherent in these products.  In addition, unlike traditional one and two part epoxies, APEX resists yellowing and discoloration of the dried film which allows for excellent touch up characteristics.  Povia APEX is also ideal for both interior and exterior applications unlike traditional epoxies.  Povia APEX is well suited for interior & exterior use at hospitals, schools, processing plants, commercial kitchens, cafeterias, bathrooms and many other areas exposed to high traffic and frequent cleaning.  Povia APEX provides excellent adhesion, superior stain resistance and abrasion resistance on a wide variety of interior and exterior substrates where maximum durability is required.  Povia APEX is also excellent for exterior DTM (direct to metal) applications.

__________________________________________________________________________________________

RECOMMENDED USES:

For virtually any properly primed interior or exterior surface of drywall, wood, plaster, masonry and metal.

SURFACE PREPARATION:

Dirt, grease, grime and any foreign material must be removed before application of new coating.  Insure surface is clean and dry.  Contact a Povia Paints representative for detailed surface preparation specifications.

APPLICATION:

Mix product thoroughly.  Apply with brush roller or airless spray. Apply when surface temperatures are at least 50 deg. and rising.  Do not thin with paint thinners.  When spraying, use a tip designed for flat wall coatings.

RECOMMENDED THINNER:

Povia 4310 does not require thinning and should be used as is, directly from the container.

RECOMMENDED PRIMER

Please contact a Povia representative for specific primer recommendations.

TECHNICAL DATA:

Finish: Satin

Pigment Type: Titanium Dioxide and inert pigments

Vehicle Type: Acrylic/Epoxy

Solvent Type: Water

% Solids By Weight: 50% +/- 2%

% Solids By Volume: 38% +/- 2%

Density: 10.47 lbs. Per gallon

Viscosity @ 75 deg. F (24 deg. C): 95 +/- 2 K.U.

Coating VOC: <75 g/l

Estimated Dry Time:  To touch 30-60 minutes ; Recoat 4-6 hours

Flash Point, Minimum: Not Flammable

Flame Spread: Class A rating on non-combustible substratum

Recommended Dry Film Thickness Per Coat: 1.0-1.5 Mils DFT.

Clean Up: Clean up drips and spills immediately using a damp cloth.  Clean tools and equipment with soap and fresh water.

Coverage (Theoretical): Coverage will depend on porosity and contour of the surface being coated.    Coverage typically averages 300-400 square feet per gallon.

Povia 4310 is water based.  Do not Freeze.

CAUTION: KEEP OUT OF REACH OF CHILDREN!

WARNING! If you scrape, sand or remove old paint, you may release lead dust.  LEAD IS TOXIC.  EXPOSURE CAN CAUSE SERIOUS ILLNESS, SUCH AS BRAIN DAMAGE, ESPECIALLY IN CHILDREN.  PREGNANT WOMEN SHOULD ALSO AVOID EXPOSURE.  Wear an NIOSH-approved respirator to control lead exposure.  Carefully clean up with a HEPA vacuum and a wet mop.  Before you start, find out how to protect yourself and your family by contacting the National Lead Information Hotline at 1-800-424-LEAD or log on to www.epa.gov/lead.

Technical data contained herein is true and accurate at the date of issue, but is subject to change without notice.  A Povia Paints representative should be contacted with any questions concerning product information or application procedures.  Our products conform to Povia quality standards, but no other warranty is expressed or implied.  Liability, if any, is limited to the replacement of product or purchase price.

## Povia Paints, Inc., 5601 Banner Dr., Ft. Myers, FL 33912  239-791-0011

www.poviapaints.com