# TECHNICAL DATA SHEET

APEX

“Clear Seal”

Acrylic/Epoxy

“HIGH PERFORMANCE CLEAR PROTECTANT”

Self-Cross Linking/Non Yellowing

Gloss Finish

4600

Specially formulated for the Florida climate

__________________________________________________________________________________________

Povia APEX “Clear Seal” Acrylic/Epoxy is an alternative to traditional, one part, pre-catalyzed waterborne epoxy finishes.  Povia APEX “Clear Seal”  is a waterborne, extremely durable, easy to use, single component acrylic/epoxy which offers many of the high performance characteristics expected from the traditional two component epoxies without the odor, pre-mixing, pot life and application difficulties inherent in these products.  In addition, unlike traditional one and two part epoxies, Povia APEX ”Clear Seal” resists yellowing and discoloration of the dried film.  Povia APEX  “Clear Seal” is designed for use as a protective finish and provides a hard, durable, mildew resistant and abrasion resistant film.  Povia APEX “Clear Seal” also provides resistance to hot tires.

__________________________________________________________________________________________

RECOMMENDED USES:

For properly prepared, concrete driveways, garage floors, patios, walkways, pool decks, warehouse floors, pavers, natural stone, brick, block, masonry walls, cement tile roofs, fiberglass doors, wood substrates, composite decking and siding.  Povia APEX is for interior and exterior use.

SURFACE PREPARATION:

Dirt, grease, grime and any foreign material must be removed before application of new coating.  Insure surface is clean and dry.  Treat for mildew using a solution of bleach and water. Oil and grease should be scrubbed with a detergent or a solution of TSP and water.

New and/or Unpainted Concrete: Allow to cure for at least 30 days prior to application and then etch with one part muriatic acid to four (4) parts water. For proper penetration and adhesion, surfaces must be etched until a porous profile is achieved. This typically requires the acid solution to stand for 10 – 15 minutes. After etching is complete, thoroughly scrub using a TSP solution or acid neutralizing detergent and then rinse clean with fresh water. Allow to dry for a minimum of 24 hours before sealing. Pressure washing is highly recommended.

Contact a Povia Paints representative for detailed surface preparation specifications.

APPLICATION:

Mix product thoroughly.  Apply with brush roller or airless spray. Apply when surface temperatures are at least 50 deg. and rising.  When spraying, use a tip designed for gloss coatings.  Do not apply when the threat of rain exists or if moisture or dew may condense on the surface prior to the sealer curing.  Do not over-apply, soak the concrete or allow the product to puddle. Two thin coats are recommended for best performance.

RECOMMENDED THINNER:

Povia 4600 does not require thinning and should be used as is, directly from the container.

TECHNICAL DATA:

Finish: Gloss

Vehicle Type: Acrylic/Epoxy

Solvent Type: Water

% Solids By Weight: 34% +/- 2%

% Solids By Volume: 32% +/- 2%

Density: 8.51 lbs. Per gallon

Viscosity @ 75 deg. F (24 deg. C): 75 +/- 2 K.U.

Coating VOC: <75 g/l

Estimated Dry Time:  To touch 30-60 minutes ; Recoat 4-6 hours; Foot traffic 24 hours; Vehicular traffic 72

hours.

Flash Point, Minimum: Not Flammable

Flame Spread: Class A rating on non-combustible substratum

Clean Up: Clean up drips and spills immediately using a damp cloth.  Clean tools and equipment with soap and fresh water.

Coverage (Theoretical): Coverage will depend on porosity and contour of the surface being coated.    Coverage typically averages 300-400 square feet per gallon.

Povia 4600 is water based.  Do not Freeze.

CAUTION: KEEP OUT OF REACH OF CHILDREN!

WARNING! If you scrape, sand or remove old paint, you may release lead dust.  LEAD IS TOXIC.  EXPOSURE CAN CAUSE SERIOUS ILLNESS, SUCH AS BRAIN DAMAGE, ESPECIALLY IN CHILDREN.  PREGNANT WOMEN SHOULD ALSO AVOID EXPOSURE.  Wear an NIOSH-approved respirator to control lead exposure.  Carefully clean up with a HEPA vacuum and a wet mop.  Before you start, find out how to protect yourself and your family by contacting the National Lead Information Hotline at 1-800-424-LEAD or log on to www.epa.gov/lead.

Technical data contained herein is true and accurate at the date of issue, but is subject to change without notice.  A Povia Paints representative should be contacted with any questions concerning product information or application procedures.  Our products conform to Povia quality standards, but no other warranty is expressed or implied.  Liability, if any, is limited to the replacement of product or purchase price.

## Povia Paints, Inc., 5601 Banner Dr., Ft. Myers, FL 33912  239-791-0011

www.poviapaints.com